## Slide 1
Challenges Related to PFAS in Packaging
Thursday, May 11, 2023

## Slide 2: Dr. Claire Sand thinks “all food packaging all the time”
Editorial Board
Associate Editor
Owner
Reviewer
National Science Foundation
Riester-Davis-Brody
Food Packaging
Lifetime Achievement Award
Recent
Awards
Adjunct
Professor
Current Leadership & Boards
Monthly
Columnist
Executive Board
IFT Fellow
Editorial Board
Claire’s mission is to enable a more sustainable food system with science and value chain innovations that more sustainably increases food shelf life and prevents food waste
35+ years of food packaging experience
Ranks innovative packaging science and value chain solutions to extend shelf life
Generates implementation roadmaps and aligns business cases
IFT Fellow, Riester-Davis-Brody life-time achievement in food packaging award recipient
Doctorate in Food Science and Nutrition at University of Minnesota
MS and BS in Packaging at Michigan State University

## Slide 3: Key Takeaways
Strong bonds in PFAS extends its existence
PFAS sources in food are from production, processing and packaging
Future Proof Packaging is needed to avoid the pitfalls of a fragmented approach
1
Industry has worked hard with a fragmented approach and alternatives to PFAS face roadblocks
2
3
4

## Slide 4: PFAS Overview
Perﬂuoroalkyl substances • All Hydrogens attached to Carbons are replaced by Fluorine
• Few degradation products and stable
Polyﬂuoroalkyl substances
  • Some Hydrogens attached to Carbons are replaced by Fluorine
• Can participate in condensation polymers such as PET, nylon • Many degradation products

## Slide 5: The Long and the Short of PFAS
Long Chain PFAS (LCPFAS)
Banned in 2016
Perfluorocarboxylic acids (PFCAs) chain length >8
Includes perfluorooctanoic acid (PFOA)
Perfluoroalkane sulfonic acids (PFSAs) chain length >6
Includes perfluorohexane sulfonic acid (PFHxS) and perfluorooctane sulfonate (PFOS)
Short Chain PFAS (SCPFAS)
Approved and became regrettable substitutes
Perfluorocarboxylic acids (PFCAs) chain length <8
Perfluoroalkane sulfonic acids (PFSAs) chain length <6

## Slide 6: LCPFAS were phased out in 2016
CAS Reg. No. 1071022-26-8
2-propenoic acid, 2-methyl-, polymer with 2-(diethylamino)ethyl 2-methyl-2-propenoate, 2-propenoic acid and 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl 2-methyl-2-propenoate, acetate
CAS Reg. No. 357624-15-8
Hexane, 1,6-diisocyanato-, homopolymer, 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluoro-1-octanol-blocked
CAS Reg. No. 1071022-26-8
2-propenoic acid, 2-methyl-, polymer with 2-(diethylamino)ethyl 2-methyl-2-propenoate, 2-propenoic acid and 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl 2-methyl-2-propenoate, acetate
CAS Reg. No. 870465-08-0
Copolymers of 2-perfluoroalkylethyl acrylate, 2-N,N-diethylaminoethyl methacrylate, glycidyl methacrylate, acrylic acid, and methacrylic acid
CAS Reg. No. 479029-28-2
Copolymer of 2-perfluoroalkylethyl acrylate, 2-(dimethylamino)ethyl methacrylate, and oxidized 2-(dimethylamino)ethyl methacrylate (2)
CAS Reg. No. 220459-70-1
Glycine, N,N-bis[2-hydroxy-3-(2-propenyloxy)propyl]-, monosodium salt, reaction products with ammonium hydroxide and pentafluoroiodoethane-tetrafluoroethylene telomer ().
CAS Reg. No. 71608–61–2
Pentanoic acid, 4,4-bis [(gamma-omegaperfluoro-C8-20-alkyl)thio] derivatives, compounds with diethanolamine
Perfluoroalkyl substituted phosphate ester acids, ammonium salts formed by the reaction of 2,2-bis[([gamma], [omega]-perfluoro C4-20 alkylthio) methyl]-1,3-propanediol, polyphosphoric acid and ammonium hydroxide.
Copolymers of 2-perfluoroalkylethyl acrylate, 2-N,N-diethylaminoethyl methacrylate, and glycidyl methacrylate
3-cyclohexene-1-carboxylic acid, 6-[(di-2-propenylamino) carbonyl]-, sodium salt, reaction products with pentafluoroiodoethane-tetrafluoroethylene telomer, ammonium salts
Diethanolamine salts of mono- and bis (1H,1H,2H,2H perfluoroalkyl) phosphates where the alkyl group is even-numbered in the range C8–C18 and the salts have a fluorine content of 52.4 percent to 54.4 percent as determined on a solids basis

## Slide 7: SCPFAS Were Phased Out In 2020
In 2020, The FDA began a 3-year phase out of 11 short-chain PFAS involved in 15 previous FCN approvals by manufacturers (Archroma, Asahi Glass, and Daikin Chemours. This includes:
CAS Reg. No. 1878204-24-0
  2-propenoic acid, 2-methyl-, 2-hydroxyethyl ester, polymer with 2-propenoic acid and 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl 2-methyl-2-propenoate, sodium salt
CAS Reg. 1440528-04-0
  Copolymer of 2-(dimethylamino) ethyl methacrylate with 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl methacrylate, N-oxide, acetate
CAS Reg. No. 1334473-84-5
  2-Propenoic acid, 2-methyl-, 2-(dimethylamino)ethyl ester, polymer with 1-ethenyl-2-pyrrolidinone and 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl 2-propenoate, acetate
CAS Reg. No. 1345817-52-8
  Butanedioic acid, 2-methylene-, polymer with 2-hydroxyethyl, 2-methyl-2-propenoate, 2-methyl-2-propenoic acid and 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl 2-methyl-2-propenoate, sodium salt
CAS Reg. No. 1206450-10-3
  2-propenoic acid, 2-methyl-, 2-hydroxyethyl ester polymer with 1-ethyenyl-2-pyrrolidinone, 2-propenoic acid and 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl 2-propenoate sodium salt
CAS Reg. No. 1071022-26-8
  2-propenoic acid, 2-methyl-, polymer with 2-(diethylamino)ethyl 2-methyl-2-propenoate, 2-propenoic acid and 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl 2-methyl-2-propenoate, acetate
CAS Reg. No. 357624-15-8
  Hexane, 1,6-diisocyanato-, homopolymer, 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluoro-1-octanol-blocked
CAS Reg. No. 1158951-86-0
  2-propenoic acid, 2-methyl-, polymer with 2-hydroxyethyl 2-methyl-2-propenoate, α-(1-oxo-2-propen-1-yl)-ω-hydroxypoly(oxy-1,2-ethanediyl) and 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl 2-propenoate, sodium salt
CAS Reg. No. 1071022-26-8
  2-propenoic acid, 2-methyl-, polymer with 2-(diethylamino)ethyl 2-methyl-2-propenoate, 2-propenoic acid and 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl 2-methyl-2-propenoate, acetate ()
2-Propenoic acid, 3,3,4,4,5,5,6,6,7,7,8,8,8-tridecafluorooctyl ester, polymer with α-(1-oxo-2-propen-1-yl)-ω-hydroxypoly(oxy-1,2-ethanediyl
CAS Reg. No. 863408-20-2 , (CAS Reg. No. 1225273-44-8
  Copolymer of perfluorohexylethyl methacrylate, 2-N,N-diethylaminoethyl methacrylate, 2-hydroxyethyl methacrylate, and 2,2'-ethylenedioxydiethyl dimethacrylate, acetic acid salt () or malic acid salt).

## Slide 8: PFAS Are Not Alone In Packaging
Other Chemicals of Concern Exist:
Phthalates
BPAs
Heavy metals
Perchlorate

## Slide 9: Selected Sources of PFAS in Packaging
Primary Packaging | Secondary & Tertiary Packaging | Ingredients | Production Environment
1
2
3
4

## Slide 10: Selected Sources of PFAS Primary Packaging
Primary Packaging | Secondary & Tertiary Packaging | Ingredients | Production Environment
Release Agents | Forming Materials | Improving Barriers | Providing Grease & Oil Resistance
For Thermoforming, blowmolding | Wetting and leveling agents, emulsifiers, foaming agents, or dispersants | Flourination of PE was approved in 1983 | Dry end coatings on paperboard and corrugated, and paper Lower the surface tension
 | Emulsifiers assist in producing Teflon examples include the use of PFOA | Now used during forming of in HPDE, PP, PET blowmolded, thermoformed containers | Wet end use on paperboard
 | Bond with functional groups such as acids and alcohols and/or take part in condensation polymerization of Nylon and PET | Primarily Polyﬂuoroalkyl substances | Coatings on hydroscopic polymers such as PLA, cellulose, starch, ethylenes, etc.
 |  | Polymers fluorinated with hexaﬂuoropropylene (HFP), tetraﬂuoroethylene (TFE), vinylidene ﬂuoride (VDF) polymers | Packaging for Pet food, bakery, FOH fried foods
1
2
3
4
Impart Improved Barrier

## Slide 11: Selected Sources of PFAS Tertiary Packaging
Primary Packaging | Secondary & Tertiary Packaging | Ingredients | Production Environment
1
2
3
4
  Packaging containing PFAS can come in contact with and then contaminate other packaging that has direct contact with food
  Migration into food can occur through secondary packaging such as labels, coatings, and cartons into food
  Handling of secondary packaging and then food in second-stage BOH/Production environments can contaminate food

## Slide 12: Selected Sources of PFAS Ingredients
Primary Packaging | Secondary & Tertiary Packaging | Ingredients | Production Environment
1
2
3
4
  Reusable packaging for bulk ingredient transport
    Includes totes, bags, liners, barrels, and bins
    Contamination of reusable totes occurs from prior use of PFAS contaminated ingredients
    Abrasion increases surface area and sites for subsequent migration
    Reuse increases migration due to contact time
  Single-use packaging for bulk ingredient transport
    Totes, bags, liners, barrels, and bins

## Slide 13: Selected Sources of PFAS Production
Primary Packaging | Secondary & Tertiary Packaging | Ingredients | Production Environment
1
2
3
4
  Equipment used to form packaging
  • Cartoners, labelers, conveyors, thermoformers, unnesters, unscramblers inhibit sticking and make production line move smoother/faster.
  Production equipment used in food processing
  • Extruders, ingredient conveyance systems, hoppers, mixers
  • PTFE (Teflon-Polytetrafluoroethylene) is use for food processing equipment
  Water and CIP cleaning agents

## Slide 14: Industry Response has been Fragmented with Drop-in Solutions

## Slide 15: Roadblocks hinder many Drop In Solutions
For many options, there are unintended consequences and/or regrettable alternatives in switching to the still approved SCPFAS
Release Agent Alternatives
  Forming Polymers Alternatives
  Improved Barrier Alternatives
  Improved Barrier Alternatives

## Slide 16
CAS Reg. No. 9011-17-0
1-propene,1,1,2,3,3,3-hexafluoro-polymer with 1,1- difluoroethene modified with a halogenated ethylene
CAS Reg. No. 25190-89-0
tetrafluoroethylene-hexafluoropropylenevinylidene fluoride copolymers
CAS Reg. No. 9011-17-0
vinylidene fluoride-hexafluoropropene copolymer
CAS Reg. No. 94228-79-2
2,3,3,4,4,5,5-Heptafluoro-1-pentene polymer with ethene and tetrafluoroethene added in 2016
CAS Reg. No. 1279108-20-1
Hexane, 1,6-diisocyanato-, homopolymer, α-[1-[[[3-[[3 (dimethylamino)propyl]amino]propyl]amino]carbonyl]-1,2,2,2-tetrafluoroethyl]-ω-(1,1,2,2,3,3,3-heptafluoropropoxy)poly[oxy[trifluoro(trifluoromethyl)-1,2-ethanediyl]]-blocked
CAS Reg. No. 464178-94-7
2-propen-1-ol, reaction products with 1,l,1,2,2,3,3,4,4,5,5,6,6-tridecafluoro-6-iodohexane, dehydroiodinated, reaction products with epichlorohydrin and triethylenetetramine as manufactured in accordance with the description in the FCN.
CAS Reg. No 464178-90-3
2-propen-1-ol, reaction products with pentafluoroiodoethane-tetrafluoroethylene telomer, dehydroiodinated, reaction products with epichlorohydrin and triethylenetetramine.
Perfluorohexane sulfonate (PFHxS)
CAS Reg. No. 69991-62-4
Perfluoropolyether dicarboxylic acid, ammonium salt.
CAS Reg. No. 200013-65-6
Diphosphoric acid, polymers with ethoxylated reduced methyl esters of reduced polymerized oxidized tetrafluoroethylene.
CAS Reg. No. 162492-15-1
Diphosphoric acid prepared by reaction of phosphorous pentoxide phosphate esters of ethoxylated perfluoroether diol
CAS Reg. No. 1314-56-3
Diphosphoric acid prepared by reaction of phosphorous pentoxide
CAS Reg. No. 2466-09-3
Diphosphoric acid prepared by reaction of phosphorous pentoxide pyrophosphoric acid.
CAS Reg. No. 328389-91-9
Fluorinated polyurethane anionic resin prepared by reacting perfluoropolyether diol (CAS Reg. No. 88645-29-8), isophorone diisocyanate (CAS Reg. No. 4098-71-9), 2,2-dimethylolpropionic acid (CAS Reg. No. 4767-03-7), and triethylamine (CAS Reg. No. 121-44-8).
Other compounds that contain flouro-based compounds at wet and dry end paperboard production and in formation of plastics
Regrettable Substitutions are a Concern
These include:

## Slide 17
• Silicone resins and elastomers as release agents
• CAS 7473-98-5, 155419-56-0, 2855-27-8, 102782-94-5, 917773-10-5
Release Agent Alternatives
Roadblocks hinder many Drop In Solutions

## Slide 18: Roadblocks hinder many Drop In Solutions
Alternatives to polymers have a host of chemicals of concern beyond PFAs
Biodegradable alternatives are very problematic
Forming Materials Alternatives

## Slide 19
Water barriers - alkyl succinic anhydride (ASA), styrene acrylic emulsion (SAE), alkyl ketene dimer (AKD) and rosin cannot be produced in sufficient volumes and are cost prohibitive now
Biopolymer PEF is promising
  Improved Barrier Alternatives
Roadblocks hinder many Drop In Solutions

## Slide 20: Roadblocks hinder many Drop In Solutions
Increased density with cellulose, carbon nanofibers, starch coatings during calendaring results in 20-30% slower production
Waxes or Polymer atomization, finishes, coatings may interfere with recycling
Removable and non-removeable plastic liners are not recyclable w/o SDO
Impart Grease & Oil Resistance Alternatives

## Slide 21: The Value Chain provides the opportunity to Future Proof Packaging
  Future Proof
  Packaging Value Chain

## Slide 22: Value Chain provides the opportunity to address
Regrettable substitutions exist
Regulations that do not align with safety
Hodge-podge of local and retailer bans
  Industry experts know that substitutions may be regrettable
  This is a costly, and time-consuming game of whack-a-mole
  Hidden data
  GRAS status is dubious
  Delayed action continues
  Reliance on voluntary abandonments
Shape-shifting supply chain
Extensive incoming inspection is costly and is not in alignment
  Snapshots do not protect brands or
  consumers

## Slide 23: Value Chain provides the opportunity to… Future Proof Packaging
Proactively Plan for the Future - Avoid kicking the can down the road with regrettable substitutions
Build a more valued safety-focused relationship with regulatory agencies
Build/rebuild Trust in all entities of the packaging value chain
Align vs Entrap value chain partners
Collective work builds a better shared future
Future-Proofed Packaging Value Chain
  Future Proof
  Packaging Value Chain
  Future Proof
  Packaging Value Chain

## Slide 24
  Adjust to Reward Significance in Relationships
  Share Work
  Manage Knowledge
  Inspire From The Top
A Future Proof Packaging Approach 4 Key Elements

## Slide 25
Collective work builds a better shared and safe future
Beyond Taskforces and to actual work
Build a Chain of Custody to instill confidence reduce fraud and add value
Deliver on shared innovations
Deliver on joint systems solutions
Work toward harmonized standards to avoid a 2-tier system in which some citizens are protected for chemicals of concern by regulations and some are not
  Share Work
A Future Proof Packaging Approach Elements

## Slide 26: Case Studies

## Slide 27: A Future Proof Packaging Approach Case Studies
    Reduce oil in contact with packaging via a systems approach using one or all of these solutions
    Reformulate fries to
        Enhanced PME-based oil resistance so that less oil is adsorbed
    BOH Processing to
    Adsorb oil prior to FOH packaging with diatomaceous earth or food grade clays
    Use a 2-phase system in which oil is drained more extensively at a station before final FOH packaging
    Non-PFAS plastic (reusable) packaging
    Package redesign to
    Employ a removeable plastic liner within FOH cartons
    FOH cartons with a sealed low point with an adsorbent substance
    FOH cartons dusted with an adsorbent substance
    PFAS sensors on packaging for value chain use
System solutions to replace for oil and grease resistance need in FOH QSR french fry cartons

## Slide 28: Key Takeaways
Strong bonds in PFAS extends its existence
PFAS sources in food are from production, processing and packaging
Future Proof Packaging is needed to avoid the pitfalls of a fragmented approach
1
Industry has worked hard with a fragmented approach and alternatives to PFAS face roadblocks
2
3
4